Liens de serrage réutilisables

Les liens de serrage réutilisables en plastique sont utilisés en cas de réouverture nécessaire.
Ces liens de serrage en plastique sont des systèmes de fermeture efficaces et durables et réutilisables. Ils sont de différentes longueurs, de 150 à 370 mm, faciles à utiliser, et garantissent des solutions de fixation sécurisées pour tout type de besoin. Les liens de serrage sont fabriqués en Nylon et offrent une grande résistance à la traction.

Caractéristiques techniques :

| Matériau | Polyamide PA-6.6 |
| --- | --- |
| Couleur | Noir |
| Température en utilisation | -40°C jusqu’à +85°C |
| Température d’installation | -10°C jusqu’à +60°C |
| Point de fusion | +260°C |
| Classe d’inflammabilité | V2 acc- a UL 94 |
| Résistance aux produits chimiques | Excellente résistance aux produits alcalins, aux produits huileux, aux solvants Résistance limitée aux acides Pas de résistance aux phénols |

Reusable cable ties

Effective and long lasting closure system, the reusable cable ties are used if reopening is required.
This is a very versatile type of releasable cable tie, as it is produced in several different sizes.  Furthermore, the positive locking features of these ties enable the user to make precise adjustments in the tension. Easy to use in a wide set of applications, the nylon cable ties provide secure fastening solutions.

Technical specifications :

| Material | Polyamide PA-6.6 |
| --- | --- |
| Colour | Black |
| Température en utilisation | -40°C up to +85°C |
| Température d’installation | -10°C up to +60°C |
| Point de fusion | +260°C |
| Classe d’inflammabilité | V2 acc- a UL 94 |
| Résistance aux produits chimiques | High resistance to bases, oils, greases, oil derivatives.Limited resistance to acids. Not resistant to phenols and to chloride solvents |

| REF | DIMENSIONS | COLOUR | RESISTANCE KG | Qty / bag |
| --- | --- | --- | --- | --- |
| LEG962102 | releasable cable tie 200x7,6 mm | black | 22 | 100 |
| LEG962101 | releasable cable tie 150x7,6 mm | black | 22 | 100 |
| LEG962103 | releasable cable tie 250x7,6 mm | black | 22 | 100 |
| LEG962104 | releasable cable tie 300x7,6 mm | black | 22 | 100 |
| LEG962105 | releasable cable tie 370x7,6 mm | black | 22 | 100 |