Intended use

Application in critical environment like semiconductor, electronic industries or high-tech industries etc.

Characteristics

- Configured with Non-woven Polypropylene/Polyethylene (ES) /Melt-blown Polypropylene (MBPP) materials

- Low particles generation and suitable for critical environments

- High bacterial filtration efficiency and low breathable resistance

- Packaged in cleanroom environment

- Solvent-safe double bag cleanroom packaging

- Head loop

General Specifications

| Item |  | Test method | Standard |
| --- | --- | --- | --- |
| Material |  | - | 18 gsm ES + 20 gsm MB + 18 gsm ES |
| Ear Loop |  | - | 30%Nylon 70%Polyester |
| Nose Piece |  | - | Plastic wire nose clip |
| Dimension | Length (cm) | Ruler | 21±0.5 |
|  | Width (cm) | Ruler | 9.5±0.2 |
| Bacterial Filtration Efficiency (%) |  | EN14683:2019+AC:2019 | >95% |
| Delta P (mmH2O) |  | EN14683:2019+AC:2019 | <6 |
| Organic Contamination |  | IEST-RP-CC003.4 | Amides and DOP free |
| Air Particle Count | ≥0.5um (counts/PC) | IEST-RP-CC003.4 | <100 |
|  | ≥0.3um (counts/PC) | IEST-RP-CC003.4 | <1000 |

Packaging and Storage

| Package/Quantity | 100pcs/Double bags, 20Bags/Case |
| --- | --- |
| Best storage Conditions | Room temperature, dry and shady |
| Shelf life | 3 years |
| Country of Origin | China |

Quality Assurance Criteria

1. Dimension and Function - Major (AQL 2.5, S-2)

•	Product dimension out of spec.

•	Fabric characteristics out of spec

•	Ear loop welding strength less than 10N for 5 seconds

2. Visual Inspection/ Attributes - Minor (AQL 4.0, L-II)

•	Foreign Material

•	Dirt

•	Holes/Tears

•	Foul odor

•	Discolor