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 SHOE COVER NON WOVEN WHITE   
113-8280

CHARACTERISTICS:

SPP shoe covers are made of 40 grams/m2 by weight, non-woven polypropylene material, commonly used in a clean environment. Non-woven shoe covers are available in white color and are manufactured, vacuum-sealed bagged in a stringent clean environment.

PHYSICAL PROPERTIES

Material					non-woven Polypropylene 40grams white No seam under the foot

Size					Universal

Length					40cm +/- 1.5cm

Height					18cm +/- 1.5cm

Opening stretched:			30cm +/- 2.5cm

Opening relaxed:				12cm +/- 1.5cm

Material Thickness			6.0 mils +/- 0.5 mils

Colour					White

Tensile strength				MD>75N/5cm;		CD>45N/5cm

Ultimate Elongation			>30 %

PACKING:

100pcs/bag, 10bags/carton case

QUALITY ASSURANCE CRITERIA:

[bookmark: _GoBack]Shoe covers are guaranteed to meet 4.0 AQL level II sampling plan per MIL-std-150E for the following defect criteria:

1.	Broken elastic band				4.	Holes/tears in fabric material 
2.	Irregular material					5.	Physical dimensions non-compliance
3.	Dirty						6. 	Not clean
							

Disclaimer: VWR wants to state that this declaration will not discharge the user from his obligation to ensure the product is suitable for the intended use. -  If there is any doubt ask us.
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