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Technical Datasheet

VWR Collection Non Sterile Cleanroom Mask with Earloop
113-6220

Intended use

	Non sterile cleanroom production or research



General Sepcification

	Item
	Test method
	Standard

	Material
	-
	28PP+23MB+21TB

	Color
	-
	Blue

	BFE (Bacterial Filtraction Efficiency)
	ASTM F2101
	98.48%

	Delta P
	MIL-M-36954C
	< 3.5

	[bookmark: _Hlk348773972]PFE(Particle Filtraction Efficiency)
	ASTM F2299
	>99%

	Particle Shedding
	IEST-RP-CC003.3 
(≥0.5μm/cu. ft.)
	Level I
196 count/ft3

	Earloop breakage test
	-
	14N for 20seconds



Material Specifications

1. 21 g/m2 TB (Thermally Bonded Polypropylene)
	Item
	Test method
	average value standard

	
	
	average value
	tolerance for average value

	Weight(g/m2)
	GB/T4669-1995
	21.00
	+/-2

	Thickness(mm)
	ASTM D1777
	/
	+/- 0.02

	Break Tensile propertities(N)
	MD
	GB/T3923.1-1997
	>60N/5cm

	
	CD
	GB/T3923.1-1997
	>20N/5cm

	Elongation rate(%)
	MD
	GB/T3923.1-1997
	>30%

	
	CD
	GB/T3923.1-1997
	>30%



[bookmark: OLE_LINK1][bookmark: OLE_LINK2]2. 23 g/m2 MB (Melt Blown Polypropylene)
	Item
	Test method
	average value standard

	
	
	average value
	tolerance for average value

	Weight(g/m2)
	GB/T4669-1995
	23.00
	+/-2

	Thickness(mm)
	ASTM D1777
	0.21
	+/- 0.02

	[bookmark: _Hlk264193532]Break Tensile propertities(N)
	MD
	GB/T3923.1-1997
	>9.5

	
	CD
	GB/T3923.1-1997
	>6.0

	Elongation rate(%)
	MD
	GB/T3923.1-1997
	>10

	
	CD
	GB/T3923.1-1997
	>10



3. 28 g/m2 PP (Spunbonded Polypropylene) 
	Item
	Test method
	average value standard

	
	
	average value
	tolerance for average value

	Weight(g/m2)
	GB/T4669-1995
	28.00
	+/-2

	Thickness(mm)
	ASTM D1777
	0.28
	+/- 0.02

	Break Tensile propertities(N)
	MD
	GB/T3923.1-1997
	>35

	
	CD
	GB/T3923.1-1997
	>24

	Elongation rate(%)
	MD
	GB/T3923.1-1997
	>60

	
	CD
	GB/T3923.1-1997
	>60



4: The product is natural rubber latex free, glass fiber and silicon free.

Dimension Specification
[bookmark: OLE_LINK3][image: 于秀娟41]

	Item
	Unit
	Spec.
	Tolerance

	A) Length
	mm
	175
	±5

	B) Width
	mm
	95
	±5

	C) Earloop Length
	mm
	175
	±10

	D) Steel nose piece length
	mm
	120
	±10



Packaging Specification
	Package/Quantity
	50pcs/PE bag, 500pcs/Case

	Best storage Conditions
	10° - 30°C

	
	40% - 75% humidity

	
	dry

	Shell Life
	3 years 

	Country of Origin
	China




Disclaimer: VWR wants to state that this declaration will not discharge the user from his obligation to ensure the product is suitable for the intended use. -  If there is any doubt ask us.
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