LABCOAT PP WATERPROOF BUTTONS - XXL

113-8268

CHARACTERISTICS:

•	Made of 48gsm PE coated non-woven Polypropylene

•	Collar

•	2 pockets

•	Longer sleeves

•	Bounded seams

•	Elastic wrist

•	Press-stud fastening

•	White colour

•	Individually packed

PHYSICAL PROPERTIES

Material					Non-woven Polypropylene coated Polyethylene 48grams/m2 white

Sizes					XXL

Length:					115cm +/-1.5cm

Width:					74cm +/- 1.5cm

Sleeve length:				56cm +/- 1.5cm

Buttons:					4 buttons

Pockets:					2 pockets

Colour					White

Tensile Strength				MD >45N/5cm;		CD >35/5cm

Ultimate Elongation			>30 %

PACKING:

1pcs/bag, 30bags/carton case

QUALITY ASSURANCE CRITERIA:

Lab coats are guaranteed to meet 4.0 AQL level II sampling plan per MIL-std-150E for the following defect criteria:

1.	Broken elastic band				4.	Holes/tears in fabric material

2.	Irregular SPP material				5.	Physical dimensions non-compliance

3.	Dirty						6. 	Not clean

Disclaimer: VWR wants to state that this declaration will not discharge the user from his obligation to ensure the product is suitable for the intended use. -  If there is any doubt ask us.

Date of issue: Feb 2020