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Certificate of Conformity

SHOE COVER NON WOVEN -PE SOLE BLUE   
113-8283

CHARACTERISTICS:

CPE (Compressed Polyethylene film) laminated SPP shoe covers are made of non-woven polypropylene material 40grams/m2 by weight, CPE film coated on the bottom is 120 grams/m2 by weight, commonly used in a clean environment. CPE laminated on the bottom shoe covers are available in white and blue color and manufactured and bagged in a stringent clean environment.

PHYSICAL PROPERTIES

Material					Non-woven Polypropylene with CPE laminated sole

Size					Universal

Length					43cm +/- 1cm

Height					16cm +/- 1cm

CPE width:				14.5cm +/- 0.5cm

Material Thickness			7.0 mils +/- 0.5 mils

Colour					Blue

Tensile strength				MD : >75N/5cm		CD : >45N/5cm

Ultimate Elongation			>30 %

PACKING:

5pcs/bundle, 10bundles/sealed bag, 4bags/inner bag, 200pcs/case
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QUALITY ASSURANCE CRITERIA:

Shoe covers are guaranteed to meet 4.0 AQL level II sampling plan per MIL-std-150E for the following defect criteria:

1.	Broken elastic band				4.	Holes/tears in fabric material 
2.	Irregular material					5.	Physical dimensions non-compliance
3.	Dirty						6. 	Not clean
							

Disclaimer: VWR wants to state that this declaration will not discharge the user from his obligation to ensure the product is suitable for the intended use. -  If there is any doubt ask us.

Date of issue: Feb 2020
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