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Technical Data Sheet


VWR® Angled Foam Mop Head, 14” two ply
Description: Knit polyester fabric laminated to 60 PPI polyester foam
Construction: Multi-layer; flame bonded/inert hi-temp adhesive 

Application: Ideal for application of disinfectants in critical environments 
Applicable part numbers:  89012-766 / 115-0199
	Attribute; (units)
	Value
	Test Method

	
	
	

	Mop weight, dry; g (mop)
	54
	CTM-004-03

	
	
	

	Sorbency in IPA/DI blend
	
	CTM-004-03

	Wet capacity; (mL/mop)
	678
	

	
	
	

	Non-volatile residue, NVR
	
	IEST-RP-CC004.2, Sec. 6.1.2

	In deionized water; (g/mop)
	0.01
	

	In isopropanol; (g/mop)
	0.02
	

	
	
	

	Particle ≥ 0.5µm; (x106/mop)
	1.3
	IEST-RP-CC004.2, Sec. 5.2

	
	
	

	Fibers > 100µm; (x103/mop)
	0.069
	IEST-RP-CC004.2, Sec. 5.2

	
	
	


	Distributed by: VWR International, LLC Radnor, PA 19087

	Manufactured by: Contec, Inc. Spartanburg, SC 29303


Important Notice

The information presented here is the result of testing and other evaluations conducted during the development of a new VWR Spec-Wipe product. This information does not constitute a specification for any existing or future product and may not be interpreted as such. This information is based on a limited sample population, and attributed values may not be similar to, or representative of, values obtained for the same attributes from a larger sampling. Where indicated, test methods used to obtain this information may be experimental in nature and may not have been shown to be repeatable and consistent for a given attribute.
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