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[bookmark: _GoBack]OVERALL PP HOOD ZIP SIZE M 
113-8261

CHARACTERISTICS:

•	Made of 40grams non-woven white Polypropylene
•	Hood
•	Waist
•	Longer sleeves & legs 
•	Elastic wrist and ankles
•	Zip fastening
•	Individually packed

PHYSICAL PROPERTIES

Material						non-woven Polypropylene 40grams/m2 

Material Thickness				0.40mm +/- 0.2 mm

Sizes						M

Colour						White

Length:						170cm +/- 2cm

Width:						67cm +/- 1.5cm	

From centre to wrist length:			88cm +/- 1cm

Tensile Strength					MD >75N/5cm;		CD >45/5cm

Ultimate Elongation				>30 %

PACKING:

1pcs/poly bag, 25pcs/case

QUALITY ASSURANCE CRITERIA:

Coveralls are guaranteed to meet 4.0 AQL level II sampling plan per MIL-std-150E for the following defect criteria:

1.	Broken elastic band				4.	Holes/tears in fabric material 
2.	Irregular SPP material				5.	Physical dimensions non-compliance
3.	Dirty						6. 	Not clean
							

Disclaimer: VWR wants to state that this declaration will not discharge the user from his obligation to ensure the product is suitable for the intended use. -  If there is any doubt ask us.

Date of issue: Feb 2020
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