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Technical DataSheet

VWR® BASIC MOBCAP SINGLE ELASTIC ESD 
EU cat. No 113-8899		
_____________________________________________________________
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CHARACTERISTICS:

•	Made of non-woven SPP fabric
•	White colour.
•	Nature Rubber Latex Free
•	Single elastic
•	Antistatic performance
•	Comply with European Commission Directive 1935/2004/EC, Regulation (EU) No.10/2011, Regulation (EU) No.2016/1416 and Regulation (EU) 2017/752.

PHYSICAL PROPERTIES

	Item
	Test method
	Standard

	Weight(g/m2)
	ISO3801
	10±1

	Break Tensile Properties
(N/5cm)
	MD
	ISO13934-1
	>15

	
	CD
	ISO13934-1
	>8

	Elongation Rate(%)
	MD
	ISO13934-1
	>30

	
	CD
	ISO13934-1
	>30

	Surface Resistance(Ω)
	EN1149-5
	<109



PRODUCTS AND DIMENSION SPECIFICATION

[image: Diagram

Description automatically generated]
Unit: CM
	ECN
	Colour
	A
	A’
	B

	113-8899
	White
	21.5
	53
	21.5

	Tolerance
	±2
	±1
	±1



Remark: A: Relax, A’: Stretch



Packaging and Storage Specifications

	Package/Quantity
	100pcs/bag, 10bags/case

	Best Storage Conditions
	Temp : 0- 50°C, 

	
	Humidity 45-85%

	
	without sunshine exposure

	Country of Origin
	China


QUALITY ASSURANCE CRITERIA:

1. Dimension and Function - Critical (AQL1.5, S-2)
•	Product dimension out of spec.
•	Fabric characteristics out of spec
•	Sonic welding strength less than 15N/5cm

2. Visual Inspection/ Attributes - Major (AQL 2.5, L-II) 
•	Foreign Material 
•	Dirt 
•	Thread ends loose or too long(over 1cm) 
•	Holes/Tears 
•	Foul odor 
•	Discolor 
•	Wrong collar tag 
•	Wrong stitch 
•	Cloth surface applied wrongly 
•	Less than 3 stitches per centimeter 

3. Visual Inspection/Attributes - Minor (AQL 4.0, L-II) 
•	Sewing sundries 
•	Elastic band end exposed 
•	Sewing end falling-off 
•	Jumping Stitch 
•	Missing stitch 
•	Unwanted folds 
•	Elastic tightness non-consistent 
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