VWR Coverall, SPP50g, antistatic, white, with hood,

zip down, elastic cuffs at ankles and waist, serged seam

INTENDED USE

Food & pharmaceutical industry, lab & research

GENERAL SPECIFICATION

| Item | Standard |
| --- | --- |
| Material | 50gsm SPP Antistatic |
| Color | White |
| Elastic | Latex free, 4mm width, white |
| Zip | Nylon |
| Surface Resistance | <1010 ohm |

MATERIAL SPECIFICATION

50gsm SPP

| Item |  | Test method | average value standard |  |
| --- | --- | --- | --- | --- |
|  |  |  | average value | tolerance for average value |
| Weight(g/m2) |  | GB/T4669-1995 | 50.00 | +/-4 |
| Break Tensile propertities | MD | GB/T3923.1-1997 | Break Tensile propertities |  |
|  | CD | GB/T3923.1-1997 | >45N/5cm |  |
| Elongation rate(%) | MD | GB/T3923.1-1997 | Elongation rate(%) |  |
|  | CD | GB/T3923.1-1997 | >30% |  |

DIMENSION

| Item | Unit | Specification |  |  |  |  |  | Tolerance |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 113-8305 | 113-8306 | 113-8307 | 113-8308 | 113-8309 | 113-8310 |  |
|  |  | M | L | XL | XXL | XXXL | XXXXL |  |
| A) Chest | cm | 61 | 63 | 68 | 72 | 75 | 79 | ±2.0 |
| B) Sleeve Outseam | cm | 87 | 91 | 93 | 94 | 96 | 100 | ±2.0 |
| C) Body Length | cm | 87 | 88 | 95 | 97 | 102 | 105 | ±2.0 |
| D) Inseam | cm | 77 | 80 | 82 | 80 | 85 | 87 | ±2.0 |
| E) Zipper | cm | 70 | 70 | 80 | 80 | 85 | 85 | ±2.0 |
| F) Wrist Relaxed | cm | 8 | 8 | 8 | 9 | 9 | 9 | ±1.0 |
| G) Ankle Relaxed | cm | 12 | 12 | 12 | 13 | 13 | 13 | ±1.0 |
| H) Full Length | cm | 160 | 163 | 170 | 172 | 180 | 187 | ±2.0 |

PACKAGE

| Package/Quantity | 1pcs/PE bag, 50pcs/Case |
| --- | --- |
| Best storage Conditions | 10° - 30°C |
|  | 40% - 75% humidity |
|  | dry |
| Shelf Life | 5 years |
| Country of Origin | China |

QUALITY ASSURANCE CRITERIA:

Coveralls are guaranteed to meet 4.0 AQL level II sampling plan per MIL-std-150E for the following defect criteria:

1.	Broken elastic band				4.	Holes/tears in fabric material

2.	Irregular SPP material				5.	Physical dimensions non-compliance

3.	Dirty						6. 	Not clean

Disclaimer: VWR wants to state that this declaration will not discharge the user from his obligation to ensure the product is suitable for the intended use. -  If there is any doubt ask us.

Date of issue: Feb 2020