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Technical DataSheet

VWR® ECO VISITOR COAT 30G PP SNAP ClOSURE ELASTIC WRIST
EU cat. No: 114-9786, 114-9787, 114-9788, 114-9789, 114-9790, 114-9791, 114-9792, 114-9793, 114-9794, 114-9795, 114-9796, 114-9797, 114-9798		
_____________________________________________________________
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CHARACTERISTICS

•	Made of 30g non-woven SPP fabric
•	White, blue and green colours options
•	Size from S to 3XL
•	Nature Rubber Latex Free
•	Snap closure with elastic wrist
•	Comply with European Commission Directive 1935/2004/EC, Regulation (EU) No.10/2011, Regulation (EU) No.2016/1416 and Regulation (EU) 2017/752.

PHYSICAL PROPERTIES

	Item
	Test method
	Standard

	Weight(g/m2)
	ISO3801
	30±4

	Break Tensile Properties
(N/5cm)
	MD
	ISO13934-1
	>40

	
	CD
	ISO13934-1
	>25

	Elongation Rate(%)
	MD
	ISO13934-1
	>30

	
	CD
	ISO13934-1
	>30





PRODUCTS AND DIMENSION SPECIFICATION
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Unit: CM
	ECN
	Colour
	Size
	A
	B
	C
	D
	E
	F
	G
	G’

	114-9786
	White
	S
	96
	63
	45
	20
	18
	48
	9
	18

	114-9787
	White
	M
	100
	66
	45
	22
	18
	50
	9
	18

	114-9788
	White
	L
	104
	69
	50
	24
	18
	52
	10
	20

	114-9789
	White
	XL
	108
	72
	50
	26
	18
	54
	10
	20

	114-9790
	White
	2XL
	112
	75
	55
	28
	18
	56
	10
	20

	114-9791
	White
	3XL
	116
	78
	55
	30
	18
	58
	10
	20

	114-9792
	Blue
	S
	96
	63
	45
	20
	18
	48
	9
	18

	114-9793
	Blue
	M
	100
	66
	45
	22
	18
	50
	9
	18

	114-9794
	Blue
	L
	104
	69
	50
	24
	18
	52
	10
	20

	114-9795
	Blue
	XL
	108
	72
	50
	26
	18
	54
	10
	20

	114-9796
	Blue
	2XL
	112
	75
	55
	28
	18
	56
	10
	20

	114-9797
	Blue
	3XL
	116
	78
	55
	30
	18
	58
	10
	20

	114-9798
	Green
	XL
	108
	72
	50
	26
	18
	54
	10
	20

	Tolerance
	±1
	±1
	±1
	±1
	±1
	±1
	±2
	±1



Remark: G: Relax, G’: Stretch

PACKAGING AND STORAGE

	Package/Quantity
	1pcs/bag, 50bags/case

	Best Storage Conditions
	Temp : 0- 50°C, 

	
	Humidity 45-85%

	
	without sunshine exposure

	Country of Origin
	China



QUALITY ASSURANCE CRITERIA

1. Dimension and Function - Critical (AQL1.5, S-2)
•	Product dimension out of spec.
•	Fabric characteristics out of spec

2. Visual Inspection/ Attributes - Major (AQL 2.5, L-II) 
•	Foreign Material 
•	Dirt 
•	Thread ends loose or too long(over 1cm) 
•	Holes/Tears 
•	Foul odor 
•	Discolor 
•	Wrong collar tag 
•	Wrong stitch 
•	Cloth surface applied wrongly 
•	Less than 6 stitches per inch 
•	Dimension tolerance not meet ±1inch for elastic and ±0.5inch for rest

3. Visual Inspection/Attributes - Minor (AQL 4.0, L-II) 
•	Sewing sundries 
•	Elastic band end exposed 
•	Sewing end falling-off 
•	Jumping Stitch 
•	Missing stitch 
•	Unwanted folds 
•	Elastic tightness non-consistent 
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