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COVERALL PP COLLAR DUAL ZIPPER XL
113-8313

CHARACTERISTICS:

[bookmark: OLE_LINK1][bookmark: OLE_LINK2]•	White SPP material 40 g/m²
•	Serged seams
•	Elasticated cuffs, ankles, hood and waist
•	Dual zipper
•	Individually packed

PHYSICAL PROPERTIES

Material					Non-woven SPP 40 g/m²

Size					XL

Length:					175cm +/- 2cm

Width:					71cm +/- 1.5cm

Sleeve length:				67cm + 2cm

Pockets:					one pocket

Colour					White

Tensile Strength				MD: >75N/5cm		CD: >45N/5cm

Ultimate Elongation			>30 %

PACKING:

1pcs/bag,25bags/carton

QUALITY ASSURANCE CRITERIA:

SPP coveralls are guaranteed to meet 4.0 AQL level II sampling plan per MIL-std-150E for the following defect criteria:

1.	Foul odor						4.	Holes/tears in fabric material 
2.	Irregular fabric material					caused by sewing machine
3.	Dirty fabric material					5.	Physical dimensions non-compliance


Disclaimer: VWR wants to state that this declaration will not discharge the user from his obligation to ensure the product is suitable for the intended use. -  If there is any doubt ask us.
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