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Product information sheet

BRADY B-7539 THERMAL TRANSFER PRINTABLE WHITE POLYESTER 

GENERAL DESCRIPTION:

B-7539 is a 50 micron Gloss White Polyester with a removable adhesive. This is an exceptionally white opaque film with a satin surface finish.

Recommended THT ribbon on B-7539: R-4900 and R-7962

PROPERTIES:

	Thickness
	substrate (polyester+clear vinyl)
	0.050 mm

	
	adhesive
	0.015 mm

	
	total
	0.065 mm

	
	
	

	Peel adhesion (ASTM D-1000)
	Stainless Steel (24 h dwell time)
	18 N / 100 mm

	
	
	

	Tack (ASTM D-2979)
	
	370 g

	
	
	

	Drop Shear (PSTC-7)
	
	15 minutes

	
	
	

	Application temperature
	
	+ 5° C

	Min. service temperature
	
	- 10° C

	Max. service temperature
	
	+100° C

	
	
	

	UV-resistance
	
	No visible effect

	
	
	


Shelf life: 2 years if stored below 80° F (26,5° C) and 60% R.H.
Shelf life is two years from the date of receipt​ for this product as long as this product is stored in its original packaging in an environment below 80° F (27° C) and 60% RH. It remains the responsibility of the user to assess the risk of using this product. We encourage customers to develop testing protocols that will qualify a product's fitness for use in their actual application.
Note:  All values shown are averages and should not be used for specification purposes.

Test data and test results contained in this document are for general information only and shall not be relied upon by Brady customers for designs and specifications, or be relied on as meeting specified performance criteria.  Customers desiring to develop specifications or performance criteria for specific product applications should contact Brady for further information.

WARRANTY

Brady products are sold with the understanding that the buyers will test them in actual use and determine for themselves their adaptability to their intended uses. Brady warrants to the buyers that its products are free from defects in material and workmanship, but limits its obligation under this warranty to replacement of the product shown to Brady's satisfaction to have been defective at the time Brady sold it.  This warranty does not extend to any persons obtaining the product from the buyers.  This warranty is in lieu of any other warranty, express or implied, including, but not limited to, any implied warranty of merchantability or fitness for a particular purpose, and of any other obligations or liability on Brady's part.  Under no circumstances will Brady be liable for any loss, damage, expense, or consequential damages of any kind arising in connection with the use, or inability to use, Brady's products.
Copyright 2008  Brady Worldwide, Inc., All Rights Reserved
Material may not be reproduced or distributed in any form without permission.
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