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CHARACTERISTICS:

•	Made of 48gsm PE coated non-woven Polypropylene
•	Collar
•	2 pockets
•	Longer sleeves 
•	Bounded seams
•	Elastic wrist
•	Press-stud fastening
•	White colour
•	Individually packed

PHYSICAL PROPERTIES

Material					Non-woven Polypropylene coated Polyethylene 48grams/m2 white

Sizes					L

Length:					100cm +/- 1.5cm

Width:					70cm +/- 1.5cm

Sleeve length:				54cm +/- 1.5cm

Buttons:					4 buttons

Pockets:					2 pockets

Colors					White

Tensile Strength				MD >45N/5cm;		CD >35/5cm

Ultimate Elongation			>30 %

PACKING:

1pcs/bag, 30bags/carton case

QUALITY ASSURANCE CRITERIA:

Lab coats are guaranteed to meet 4.0 AQL level II sampling plan per MIL-std-150E for the following defect criteria:

1.	Broken elastic band				4.	Holes/tears in fabric material 
2.	Irregular SPP material				5.	Physical dimensions non-compliance
3.	Dirty						6. 	Not clean
							

Disclaimer: VWR wants to state that this declaration will not discharge the user from his obligation to ensure the product is suitable for the intended use. -  If there is any doubt ask us.
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