CHARACTERISTICS:

•	Made of non-woven SPP fabric

•	Multiple colours option from white, blue, green to red.

•	Nature Rubber Latex Free

•	Double elastic

•	Detectable

•	Comply with European Commission Directive 1935/2004/EC, Regulation (EU) No.10/2011, Regulation (EU) No.2016/1416 and Regulation (EU) 2017/752.

PHYSICAL PROPERTIES

| Item |  | Test method | Standard |
| --- | --- | --- | --- |
| Weight(g/m2) |  | ISO3801 | 10±1 |
| Break Tensile Properties (N/5cm) | MD | ISO13934-1 | >15 |
|  | CD | ISO13934-1 | >8 |
| Elongation Rate(%) | MD | ISO13934-1 | >30 |
|  | CD | ISO13934-1 | >30 |

PRODUCTS AND DIMENSION SPECIFICATION

Unit: CM

| ECN |  | 113-8895 | 113-8896 | 113-8897 | 113-8898 | 113-8895 White |
| --- | --- | --- | --- | --- | --- | --- |
| Colour |  | White | Blue | Green | Red |  |
| Dimension | A | 20 | 20 | 20 | 20 | 20 |
|  | A’ | 53 | 53 | 53 | 53 | 53 |
|  | B | 21.5 | 21.5 | 21.5 | 21.5 | 21.5 |

Remark: A: Relax, A’: Stretch

Packaging and Storage Specifications

| Package/Quantity | 100pcs/bag, 10bags/case |
| --- | --- |
| Best Storage Conditions | Temp : 0- 50°C, |
|  | Humidity 45-85% |
|  | without sunshine exposure |
| Country of Origin | China |

QUALITY ASSURANCE CRITERIA:

1. Dimension and Function - Critical (AQL1.5, S-2)

•	Product dimension out of spec.

•	Fabric characteristics out of spec

•	Sonic welding strength less than 15N/5cm

2. Visual Inspection/ Attributes - Major (AQL 2.5, L-II)

•	Foreign Material

•	Dirt

•	Thread ends loose or too long(over 1cm)

•	Holes/Tears

•	Foul odor

•	Discolor

•	Wrong collar tag

•	Wrong stitch

•	Cloth surface applied wrongly

•	Less than 3 stitches per centimeter

3. Visual Inspection/Attributes - Minor (AQL 4.0, L-II)

•	Sewing sundries

•	Elastic band end exposed

•	Sewing end falling-off

•	Jumping Stitch

•	Missing stitch

•	Unwanted folds

•	Elastic tightness non-consistent

Date of Issue: Mar 8, 2022