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 SHOE COVER ANTISKID PP LAMINATED WHITE   
113-8287

CHARACTERISTICS:

Non-skid PE film laminated SPP shoe covers are made of PE non-skid film 20grams/m2 coated non-woven polypropylene material 40grams/m2, commonly used in a clean environment. PE non-skid laminated shoe covers are available in purple color and manufactured and bagged in a stringent clean environment (workshop closed and installed a air-conditioner).

PHYSICAL PROPERTIES

Material					non-skid PE film laminated non-woven Polypropylene 

Material Weight       			60 g/m2

Size					42cm

Length					42 cm +/- 1.5 cm

Height					17 cm +/- 1 cm

Opening					29 cm +/- 2.5cm stretched		13 cm +/- 1.5 cm relaxed

Colour					White

Tensile strength				MD>75N/5CM		CD>45N/5CM

Ultimate Elongation			>30%

PACKING:

10pcs/bundle, 30bundles/bag, 300pcs/case

QUALITY ASSURANCE CRITERIA:

Shoe covers are guaranteed to meet 4.0 AQL level II sampling plan per MIL-std-150E for the following defect criteria:

1.	Broken elastic band				4.	Holes/tears in fabric material 
2.	Irregular material					5.	Physical dimensions non-compliance
3.	Dirty						6. 	Not clean
							

Disclaimer: VWR wants to state that this declaration will not discharge the user from his obligation to ensure the product is suitable for the intended use. -  If there is any doubt ask us.

Date of issue: Feb 2020
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