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 VWR Lab coat,
SPP45, white, single collar, buttons , two pockets, open cuffs

INTENDED USE

	[bookmark: _GoBack]Food & pharmaceutical industry, lab & research



GENERAL SPECIFICATION

	Item
	Standard

	Material
	45gsm SPP

	Color
	White

	Elastic
	Latex free, 3mm width, white

	Button
	Nylon



MATERIAL SPECIFICATION

45gsm SPP
	Item
	Test method
	average value standard

	
	
	average value
	tolerance for average value

	Weight(g/m2)
	GB/T4669-1995
	45.00
	+/-2

	Break Tensile properties(N)
	MD
	GB/T3923.1-1997
	>75N/5cm

	
	CD
	GB/T3923.1-1997
	>45N/5cm

	Elongation rate(%)
	MD
	GB/T3923.1-1997
	>30%

	
	CD
	GB/T3923.1-1997
	>30%





DIMENSION
[image: ]

	Item
	Unit
	Specification
	Tolerance

	
	
	113-8297
	113-8298
	113-8299
	113-8302
	113-8303
	113-8304
	

	
	
	M
	L
	XL
	XXL
	XXXL
	XXXXL
	

	A) Total Length
	cm
	100
	103
	105
	108
	112
	115
	±2.0

	B) Chest
	cm
	66
	68
	69.5
	70.5
	72
	75
	±2.0

	C) Sleeve Length
	cm
	58
	±2.0

	D) Wrist
	cm
	16.5
	±1.0

	E) Buttons Distance
	cm
	17
	±1.0

	F) Pockets Width
	cm
	16.5
	±1.0

	G) Pockets Length
	cm
	17.5
	±1.0



PACKAGE

	Package/Quantity
	1pcs/PE bag, 50pcs/Case

	Best storage Conditions
	10° - 30°C

	
	40% - 75% humidity

	
	dry

	Shelf Life
	5 years 

	Country of Origin
	China





QUALITY ASSURANCE CRITERIA:

Lab coats are guaranteed to meet 4.0 AQL level II sampling plan per MIL-std-150E for the following defect criteria:

1.	Broken elastic band				4.	Holes/tears in fabric material 
2.	Irregular SPP material				5.	Physical dimensions non-compliance
3.	Dirty						6. 	Not clean
							

Disclaimer: VWR wants to state that this declaration will not discharge the user from his obligation to ensure the product is suitable for the intended use. -  If there is any doubt ask us.

Date of issue: Feb 2020
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