Sterile Garment Set CAT III TYPE 5/6 L

Sterile single-use clean room garment set, PPE Cat III , Type 5 and 6 ,  including overall, hood, boot covers and sleeve protectors, all made from breathable SMS 60g fabric, aseptic donning design

Intended use

Sterile cleanroom production or research

General Specification

| Item | Test method | Standard |
| --- | --- | --- |
| Material | - | 60g SMS + 100g antiskid PU film for sole |
| Color | - | White |
| Zipper | - | Nylon |
| Elastic | - | Thumb loop : latex free Rest : latex |
| BFE (Bacterial Filtraction Efficiency) | ASTM F2101 | >90.5% |
| Particle Shedding | IEST-RP-CC003.3 (≥0.5μm/cu. ft.) | 409 Level I |
| Sterilization | ISO11137 | SAL10-6 |
| Surface resistivity (Ω) | EN1149-1:2008 | <2.5*109 |

Material Specifications

1. 60gsm SMS

| Item |  | Test method | average value standard |  |
| --- | --- | --- | --- | --- |
|  |  |  | average value | tolerance for average value |
| Weight(g/m2) |  | GB/T4669-1995 | 60.00 | +/-3 |
| Thickness(mm) |  | ASTM D1777 | 0.184 | +/- 0.02 |
| Break Tensile propertities(N) | MD | ASTM D5034 | >60 |  |
|  | CD | ASTM D5034 | >35 |  |
| Elongation rate(%) | MD | ASTM D5034 | >30 |  |
|  | CD | ASTM D5034 | >30 |  |
| Tear prosperities | MD | ISO9073-4 | >30 |  |
|  | CD | ISO9073-4 | >30 |  |
| Hydrostatic press test (mmH2O) |  | AATCC127 | >450 |  |
| Air permeability test (mm/s) |  | ISO9073-15 | >200 |  |
| Surface resistivity (Ω) |  | EN1149-1:2008 | <2.5*109 |  |

2. 100g antiskid PU film for sole

| Item |  | Test method | average value standard |  |
| --- | --- | --- | --- | --- |
|  |  |  | average value | tolerance for average value |
| Thickness |  | ASTM D1777 | 0.13mm | +/-0.05mm |
| Slip resistance | DRY | ASTM F1677 | >0.8 |  |
|  | WET | ASTM F1677 | >0.69 |  |
|  | OIL | ASTM F1677 | >0.42 |  |
| Surface resistivity |  | EN1149-1:2006 | <1010 |  |

Dimension Specification

| EU Cat. No. | SIZE | A | B | C | D | E | F | G | H | I | J | K |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 113-7875 | S | 166 | 57 | 85 | 25 | 8/18 | 12/24 | 29 | 70 | 35 | 15 | 42 |
| 113-7876 | M | 169 | 60 | 86 | 25 | 8/18 | 12/24 | 32 | 70 | 35 | 15 | 42 |
| 113-7877 | L | 176 | 63 | 90 | 25 | 8/18 | 12/24 | 35.5 | 70 | 40 | 15 | 42 |
| 113-7878 | XL | 178 | 66 | 92 | 25 | 9/20 | 13/26 | 36.5 | 75 | 40 | 15 | 42 |
| 113-7879 | XXL | 186 | 74 | 98 | 25 | 9/20 | 13/26 | 39 | 75 | 45 | 15 | 42 |
| 113-7880 | XXXL | 192 | 79 | 99 | 25 | 9/20 | 13/26 | 43 | 75 | 45 | 15 | 42 |
| Tolerance |  | ±3 | ±2 | ±3 | ±1 | ±1/±2 | ±1/±2 | ±1 | ±2 | ±2 | ±1 | ±1 |

Packaging Specification

| Package/Quantity | 1pcs/pe bag/pe bag, 20pcs/case liner /case |
| --- | --- |
| Best storage Conditions | 0° - 50°C |
|  | 45% - 65% humidity |
|  | dry |
| Shell Life | 5 years |
| Country of Origin | China |

Product Compliance:

ISO 13485:2003 Medical device-Quality management system-requirements for regulatory

EN 13688:2013 Protective clothing – general requirements

EN ISO13982-1:2004 +A1:2010 Protective clothing for use against solid particulates-Part1: Performance requirements for chemical protective clothing providing protection to the full body against airborne solid particulates

EN 13034:2005+A1:2009 Protective clothing against liquid chemicals – Performance requirements for chemical protective clothing offering limited protective performance against liquid chemicals

EN 1149-5:2008 Protective clothing – Electrostatic properties – Part 5: Material performance and design requirements

Disclaimer: VWR wants to state that this declaration will not discharge the user from his obligation to ensure the product is suitable for the intended use. -  If there is any doubt ask us.

Date of issue: Dec 2021