OVERALL PP COLLAR ZIP SIZE XXL

113-8260

CHARACTERISTICS:

•	Made of 40grams non-woven white Polypropylene

•	Collar

•	Waist

•	Longer sleeves & legs

•	Elastic wrist and ankles

•	Zip fastening

•	Individually packed

PHYSICAL PROPERTIES

Material						non-woven Polypropylene 40grams/m2

Material Thickness				0.40mm +/- 0.2 mm

Sizes						XXL

Colour						White

Length:						178cm +/- 2cm

Width:						73cm +/- 1.5cm

From centre to wrist length:			94cm +/- 1cm

Tensile Strength					MD >75N/5cm;		CD >45/5cm

Ultimate Elongation				>30 %

PACKING:

1pcs/poly bag, 25pcs/case

QUALITY ASSURANCE CRITERIA:

Coveralls are guaranteed to meet 4.0 AQL level II sampling plan per MIL-std-150E for the following defect criteria:

1.	Broken elastic band				4.	Holes/tears in fabric material

2.	Irregular SPP material				5.	Physical dimensions non-compliance

3.	Dirty						6. 	Not clean

Disclaimer: VWR wants to state that this declaration will not discharge the user from his obligation to ensure the product is suitable for the intended use. -  If there is any doubt ask us.

Date of issue: Feb 2020