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BEARD COVER WHITE + ELASTIC
113-8254

CHARACTERISTICS:

Beard masks are made of 12 grams/m2 by weight, non-woven polypropylene material, commonly used in a clean environment. Beard covers are manufactured and vacuum sealed in a stringent clean environment.

PHYSICAL PROPERTIES

Material					non-woven Polypropylene 12g, white
Elastic					latex free

Size					Large

Stretch Length				45+/-1cm

Material Thickness			2.0 mils +/- 0.2mil

[bookmark: _GoBack]Colour					White

Tensile Strength				MD>16N/5cm;	CD>10N/5cm

Ultimate Elongation			>30%

PACKING:

100pcs/bag, 10 bags/case

QUALITY ASSURANCE CRITERIA:

Beard covers are guaranteed to meet 4.0 AQL level II sampling plan per MIL-std-150E for the following defect criteria:

1.	Broken elastic band				4.	Holes/tears in fabric material 
2.	Irregular SPP material				5.	Physical dimensions non-compliance
3.	Dirty						6. 	Not clean
							

Disclaimer: VWR wants to state that this declaration will not discharge the user from his obligation to ensure the product is suitable for the intended use. -  If there is any doubt ask us.

Date of issue: Feb 2020
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