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 SHOE COVER ANTISKID SPP BLUE   
113-8286

CHARACTERISTICS:

SPP shoe covers non-skid are made of 40 grams/m2 by weight, non-woven polypropylene material printed white latex lines, commonly used in a clean environment. Non-woven shoe covers are available in blue color. SPP shoe covers are manufactured, vacuum-sealed bagged in a stringent clean environment.

PHYSICAL PROPERTIES

Material					non-woven Polypropylene printed white latex lines

Size					XL

Length					46 cm +/- 1.5 cm

Height					20 cm +/- 1.5cm

Material Thickness			6.0 mils +/- 0.5 mils

Colour					Blue with printed white latex lines

Tensile strength				MD: >75N/5cm		CD: >45N/5cm

Ultimate Elongation			>30%

PACKING:

[bookmark: _GoBack]10pcs/bundle, 10bundles/bag, 10bags/case

QUALITY ASSURANCE CRITERIA:

Shoe covers are guaranteed to meet 4.0 AQL level II sampling plan per MIL-std-150E for the following defect criteria:

1.	Broken elastic band				4.	Holes/tears in fabric material 
2.	Irregular material					5.	Physical dimensions non-compliance
3.	Dirty						6. 	Not clean
							

Disclaimer: VWR wants to state that this declaration will not discharge the user from his obligation to ensure the product is suitable for the intended use. -  If there is any doubt ask us.

Date of issue: Feb 2020
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