VOLTEC® Cleanroom Mask

with Knitted Earloops

Catalog # 62692

(old Tecnol # CR40-500)

From Kimberly-Clark’s collection of industrial face masks, the VOLTEC® Cleanroom Mask with Knitted Earloops is a  blue,  pleat style face mask which offers good filtration of particles and bacteria with good breathability.

Face Mask Construction:	 Utilizing Sontec II Ultra Sonic Bonding

1. Binding				- White, Spunlaced Polyester

2. Nosepiece				- Fully Enclosed, Soft, Malleable Aluminum

3. Outer Facing			- Blue, Wet-Laid Polyester/Cellulose

4. Inner Facing			- White, Wet-Laid Polyester/Cellulose

5. Filter Media			- White, Meltblown Polypropylene

6. Earloops				- White, Knitted Polyester/Polyurethane

Packaging:				50 Masks Per Bag

10 Bags Per Lined Case (500 total/case)

Particle Filtration Efficiency @ 0.1 micron				     >90%

Bacterial Filtration Efficiency @ 3.0 micron	                                     >90%

Differential Pressure in mm H2O @ 8 LPM flow rate		     1.70

For Further Information Contact:

PARTNERS IN QUALITY® AT 1-800-KC HELPS (1-800-524-3577)

All testing was completed by an independent testing facility.  Test methods are available upon request.

PFE:  Tested according to ASTM F1215-89

BFE:  Tested according to MIL-M-36954C

(P:    Tested according to MIL-M-36954C

Product Data Sheet - 1/13/99