CR CLASSICTM Face Mask

w/Knitted Earloops

Catalog # 62465

(old Tecnol # 45175)

From Kimberly-Clark’s World Class Collection of face masks, the CR CLASSICTM Face Mask with Knitted Earloops is a pleat style mask.  Used in Class 10 or higher cleanroom environments.*

Face Mask Construction:	 Utilizing Sontec II Ultra Sonic Bonding

1. Binding				- White, Hydroentangled Polyester

2. Nosepiece				- Fully Enclosed, Soft, Malleable Aluminum

3. Outer Facing			- Clear, Polyethylene, Apertured Film

4. Inner Facing			- White BiCoSof™ Fabric

5. Filter Media			- White,High Efficiency, Meltblown Polypropylene

6. Earloops				- White, Tubular Knitted Polyester/Polyurethane

Packaging:				50 Masks Per Double Bag

10 Bags Per Case (500 total/case)

Particle Filtration Efficiency @ 0.1 micron				99.5%

Differential Pressure in mm H2O @ 8 LPM flow rate		1.33

Bacterial Filtration Efficiency @ 3.0 micron				98.7%

For Further Information Contact:

PARTNERS IN QUALITY® AT 1-800-KC HELPS (1-800-524-3577)

All testing was completed by an independent testing facility.  Test methods are available upon request.

PFE:  Tested according to ASTM F1215-89

BFE:  Tested according to MIL-M-36954C

(P:    Tested according to MIL-M-36954C

*Statement based on sales of product into fabs.  We recommend testing the product for use in your facility.

Product Data Sheet - 10/1/98